## Slide 1
Chemical Reaction Engineering – II (CL24303)
MO2026

## Slide 2
Fluidized Bed
Fluidized Catalytic Cracking (FCC)
Parameter | Typical Value
Reactor temp | 490–550 °C
Regenerator temp | 650–750 °C
Pressure | 1.5–3 atm
Catalyst/oil ratio | 5.5 (wt/wt)
Residence time | 2–5 seconds
Catalyst- Y-Zeolites

## Slide 3
Fluidized Bed
Fluidized Catalytic Cracking (FCC)
Parameter | Typical Value
Reactor temp | 480–550 °C
Regenerator temp | 650–715 °C
Pressure | 1.5–3 atm
Catalyst/oil ratio | 5.5 (wt/wt)
Residence time | 2–5 seconds
Catalyst- Y-Zeolites (Faujasite)
Size- 50-100 μm
Vogt, E.T. and Weckhuysen, B.M., 2015. Chemical Society Reviews, 44(20), 7342-7370
Pressure balance
Thermal Balance

## Slide 4
Y-Zeolites of Faujasite (FAU) Framework
Fluidized Catalytic Cracking (FCC)
Components
Zeolite (Active Components) -15-50%
Active Material (Support) – Amorphous Silica-Alumina
Binder – Silica sol or alumina to hold active matter and provide mechanical strength
Filler – Clay (Kaolin) for physical and thermal stability
https://courses.ems.psu.edu/fsc432/node/713
Particle Density – 1.2-1.5 g/cc
Bulk Density – 0.65-0.96 g/cc

## Slide 5
Catalyst Particle
Active Sites
A
A
B
B
Catalyst Pore
1. Transport of ‘A’ to pore mouth from bulk
7. Transport of ‘B’ from pore mouth to bulk
A
B
6. Diffusion of ‘B’ from active site to pore mouth
2. Diffusion of ‘A’ to active site from pore mouth
3. Adsorption of A
4. Surface reaction of A to B
5. Desorption of B
Steps in Catalytic Reaction
Sponge
Soyabean Nugget
Rasgulla

## Slide 6: Catalyst Shapes
Wagon wheel
Monolith

## Slide 7: Effects of Catalyst Shapes

## Slide 8: Catalyst Preparation

## Slide 9
Sample Degassing
Test Station
N2 + He
Carrier Gas
Adsorbate
BET Measurement

## Slide 10
A+B
C
Interparticle Void
Intraparticle Void
Density

## Slide 11
Pore Volume – Mercury Intrusion Method
Ritter and Drake

## Slide 12
Module 3
Module 2
Module 1
Active Sites
CA,b
Catalyst Particle
Catalyst Pore
1. External Mass Transfer of ‘A’ to pore mouth from bulk
7. External Mass Transfer of ‘B’ from pore mouth to bulk
CB,s
6. Internal Diffusion of ‘B’ from active site to pore mouth
2. Internal Diffusion of ‘A’ to active site from pore mouth
3. Adsorption of A
4. Surface reaction of A to B
5. Desorption of B
Catalytic Reaction
Intrinsic rate kinetics
(LHHW)
CA
CA,b
CA,s
CB

## Slide 13
CH4 is weakly adsorbed as rate is independent of pM
Benzene is adsorbed as rate depends on pB
Hydrogen concentration increases rate that depends on pH
Toluene concentration doesn’t affect rate at high pT
Toluene concentration increases rate at low pT

## Slide 14
Propose a mechanism
Assume a rate-limiting step
Site-Balance
Derive Rate Law
2. Surface Reaction
1. Adsorption
Dissociative
Non-Dissociative (Molecular)
Single Site
Multi-Site
Eley-Rideal
3. Desorption
Or Or OR
Pseudo Steady State Hypothesis (PSSH) OR OR
Express Cv (Concentration of vacant sites)
Determination of parameters and comparison with experiments
No
Yes
Driving Force or Shift from equilibrium
Kinetic Term
Resistance
LHHW Kinetics
CSTR
Packed Bed Reactor
Mechanistic
Kinetic Modelling

## Slide 15: Reactor Design using LHHW Kinetics
It is assumed that for a certain catalyst, the pore diffusion can be neglected. How much of that catalyst is needed in a packed-bed reactor for 80% conversion of 1000 m3/hr of pure gaseous A (CAb = 100 mol/m3) if the stoichiometry and rates are given by:
, [Ans: 64.3 kg]
Use the design equation for the Packed Bed Reactor for

## Slide 16
Diffusion in Catalyst Pores
A
A
A
A
A
Bulk Diffusion
A
A
A
A
Surface Diffusion
A
A
A
A
A
Knudsen Diffusion
A
dpore
Bosanquet Equation
Proportionality Factor
Jump Length
Correlation Time
Pellet Porosity (0.2-0.5)
Constriction Factor
Tortuosity (2-5)

## Slide 17
Diffusion in Catalyst Pores
A
A
A
A
A
Bulk Diffusion
A
A
A
A
Surface Diffusion
A
A
A
A
A
Knudsen Diffusion
A
Valid for equimolar counter diffusion

## Slide 18
2b
Assumptions
Mass transfer only due to diffusion. Mass flux
Consumption of A due to
Steady-state
1-D mass transfer
y
x
-b
0
b
Diffusion in Catalyst Pores
Scaled variables
Boundary Conditions
Thiele Modulus
Weak adsorption at high temperature

## Slide 19
Centre
Pore Mouth
Chart: ξ
ξ
y
x
0
b
y
x
-b
0
b
Diffusion in Catalyst Pores
ξ
y
x
0
b
ξ
But which to be used for reactor design?

## Slide 20
Diffusion in Catalyst Pores
1st order Reaction
Flat
Sphere
Cylinder
order
Or CA,bulk
Rate constant
Effective diffusivity
Length Scale
nth order Reaction

## Slide 21
Diffusion in Catalyst Pores
CAs
CAb
Film
CA
If
If
No step 1
Experimentally measured
Experimentally unmeasurable
i.e.,

## Slide 22
Shape |  |  | η
Flat |  |  | 
Sphere |  |  | 
Cylinder | - |  | 
Shape |  |  | η
Flat |  |  | 
Sphere |  |  | 
Cylinder | - |  | 
Diffusion in Catalyst Pores

## Slide 23
CA,b
CB,b
Catalyst Pore
1. Mass Transfer of ‘A’ to pore mouth from bulk
7. Mass Transfer of ‘B’ from pore mouth to bulk
CB,s
6. Diffusion of ‘B’ from active site to pore mouth
2. Diffusion of ‘A’ to active site from pore mouth
3. Adsorption of A
4. Surface reaction of A to B
5. Desorption of B
Catalytic Reaction
Langmuir-Hinshelwood-Hougen-Watson (LHHW) kinetics
CB
CA
CA,s
Role
Enhances the rate of
reaction without altering the Thermodynamics
Binds reactants/products by adsorption (chemisorption)
Characterization
Surface Area (BET)
Pore Volume (Mercury Intrusion)
CA
CA,b
Distance
CA,s
CA
Film
Bulk
Kinetic Limited (Slow) reaction -
Mass transfer Limited (Fast) reaction -

## Slide 24
Diffusion in Catalyst Pores
Kinetic Controlled
Strong Pore Diffusion controlled
For
Falsified kinetics
Under strong pore diffusion limitation -
Active sites decrease

## Slide 25
Deactivation of Catalyst
Active Sites
Access to Active Sites
a(t)
t
Specific Decay Constant (function of Temperature)
Concentration dependent
‘Time-on-stream’ experiments

## Slide 26
Catalyst Deactivation
Chemical
Thermal
Mechanical
Poison
Vapour Formation
Vapour-Solid and Solid-Solid Reactions
Fouling
Attrition/Crushing
Sintering
Deactivation of Catalyst

## Slide 27
Modes of Deactivation of Catalyst - Sintering (Ageing)
Loss of active site due to high temperature leading to Crystal Agglomeration, growth of metal deposits, change in surface morphology
Metal Agglomeration
Pore Blockage
Solution?
Maintain temperature
Catalyst design with stronger metal-support interaction

## Slide 28
Modes of Deactivation of Catalyst - Fouling (Carbon/Coke)
Deposition of species (carbon) on active sites
Solution?
High Pressure 2000-3000 kPa (20-30 atm)
  Suppresses side reactions to prevent the formation of smaller hydrocarbons that produce carbon
Hydrogen-rich streams to promote methanation reaction (CH4 formation) (Fischer-Tropsch synthesis)
Catalyst regeneration with short contact time – Better Reactor Design
Polymeric/ graphitic carbon film
(Typical with hydrocarbons at high temperature )
Boudouard reaction
,

## Slide 29
Modes of Deactivation of Catalyst- Poisoning
Chemisorption of molecules on active sites. It may be a reactant/ product as well
Typical poisons are – S, CO, Heavy metals (Pb, Hg, As, Cd), Halides (Chlorides, Fluorides) Nitrogen-rich compounds, and even moisture
Poisoning of the support by Sulphur for the hydrogenation of ethylene
Solution?
Feed Purification – Removal of S, heavy metals
Guard Bed

## Slide 30
Industrial Application | Catalyst Type | Typical Lifespan | Primary Cause of Failure | Reactor Type
Ammonia Synthesis | Promoted Iron (Fe) | 5–10+ years | Thermal sintering, oxygen poisoning | Fixed Bed
Sulfuric Acid Production | Vanadium Pentoxide (V₂O₅) | 5–10 years | Dust/ash accumulation, structural breakdown | Fixed Bed
Automotive Emissions | Platinum, Palladium, Rhodium (Pt/Pd/Rh) | 10–15 years | Thermal degradation, engine oil poisoning | Monolith
Steam Methane Reforming | Nickel (Ni) on Alumina | 3–5 years | Carbon deposition (coking), sintering | Tubular Fixed Bed
SCR (Power Plants) | Titanium/Vanadium (TiO₂/V₂O₅) | 3–5 years | Fly ash erosion, arsenic/alkali poisoning | Monolith / Honeycomb
Methanol Synthesis | Copper-Zinc-Alumina (Cu/ZnO/Al₂O₃) | 2–5 years | Severe thermal sintering, trace sulfur | Fixed Bed
Hydrotreating | Cobalt-Molybdenum (CoMo) / Nickel-Molybdenum (NiMo) | 2–4 years | Sulphur/nitrogen saturation, metal deposition | Fixed Bed
Ethylene Oxide | Silver (Ag) on Alumina | 2–3 years | Thermal sintering, chemical poisoning | Multi-tubular Fixed Bed
Catalytic Reforming | Platinum-Rhenium (Pt-Re) | 1–3 years | Rapid coking (requires frequent regeneration) | Moving or Fixed Bed
Fluidized Catalytic Cracking | Zeolites (Y-Zeolite) | Seconds per cycle; Months total life | Coking (seconds), hydrothermal sintering (months) | Fluidized Bed
Life-Time of Industrial Catalysts
Rate of Deactivation Fixed (Packed) Bed Reactor
Rate of Deactivation Fluidized Bed Reactor

## Slide 31
Summary
Q7 of Tutorial 4
Q8 of Tutorial 4
Reaction – Diffusion Equation
Activity, Selectivity, Productivity, and Stability

## Slide 32
Flow
Effective Diffusivity
Kinetic controlled
Strong Pore Diffusion controlled
Gas Solid Catalytic Reaction

## Slide 33
Diffusion of knowledge in human brain
The lesser the diffusional resistance of the brain, the greater is the transfer and retention of knowledge
Deactivation
Distractions
Company
Motivation
Addictions
ξ
Kinetic Controlled
Strong Pore Diffusion controlled

## Slide 34
Effect of Mass Transfer Limitations on Reactor Design
Test Tube
No Transport (mass, heat, and fluid) limitation
Only kinetics (i.e., Concentration and Temperature)
Overall Effectiveness Factor
Wish list-
Internal pore
diffusion resistance
External
mass transfer resistance
So…
If
manageable Fixed Bed Reactor
too high Fluidized Bed Reactor / Slurry Reactor

## Slide 35
Effect of Mass Transfer Limitations on Reactor Design

## Slide 36
Gas/Solid Reactors – Fixed Bed Reactor
Multi-Tubular
Inter-stage cooling
Pros-
Stationary/fixed solids
Low operating velocity
Nearly plug flow of fluids
Bigger particles (~mm)
Simpler design
Applications – Diesel Hydrodesulphurization (DHDS)
Cons-
Poor heat and mass transfer
Lower throughput
Cannot operate under high deactivation
Higher ΔP

## Slide 37
Gas/Solid Reactors – Fluidized Bed Reactor
Pros-
High operating velocity
Superior heat and mass transfer
Lower ΔP
Suitable under mass transfer limited limitation and deactivation
Applications – Fluidized Catalytic Cracker (FCC)
Cons-
Complicated Design
Difficult to scale up
High Attrition
Smaller particles (~ 50-500μm)

## Slide 38
Module 4
Module 2
Module 1
Active Sites
A
A
B
B
Catalyst Particle
Catalyst Pore
1. External Mass Transfer of ‘A’ to pore mouth from bulk
7. External Mass Transfer of ‘B’ from pore mouth to bulk
A
B
6. Internal Diffusion of ‘B’ from active site to pore mouth
2. Internal Diffusion of ‘A’ to active site from pore mouth
3. Adsorption of A
4. Surface reaction of A to B
5. Desorption of B
Catalytic Reaction
Intrinsic rate kinetics
(LHHW)
n- Total species
m- Total reactants